Road to CAC2022, 21st July
Clay classification using a handheld
laser-induced breakdown spectrometer
Kozin Artyom M.1, Labutin Timur A.1, Korshunov Dmitry M.2
1. Department of Chemistry, Lomonosov Moscow State University
2. Department of Geology, Lomonosov Moscow State University

---
Introduction
- In-field control of mining is important, as it allows for major financial losses to be avoided in a simple way
- Needs to be efficient and rapid, simple and portable, thus, most likely, without any chemical treatment
- Portable LIBS devices which appeared in XXI century are the promising candidates for the job

---
Goals
- Test the capabilities of a portable LIBS device
- Test how well PCA can be applied to classify clay rocks
- Compare using Ar to not using Ar during the lazing stage of clay samples analysis

---
The samples
- Clay from different depths
- Mostly kaolinite, calcite and 4 samples of lab-fabricated kaolinite, 29 samples total
12 mm
Hydraulic press, ~40 atm
mortar and pestle
2~3 mm

---
Lazing
- SciAps Z-300 was employed, with and without Ar canisters in 2 separate data sets
- 3 lazing points on the sample in total
Wavelength (nm)

---
PCA
- Using each waveband as a coordinate axis, we conducted PCA on the sample sets.
- Also, we conducted the PCA on modified sets in an attempt to remove the influence of
  non-characteristic but very prominent signals of Al, Si and their common compounds present in all samples.
We decided that 4 PCs is enough
Cuts to the spectra are in red:
308~310, 394~398, 464.5~473, 484~493 nm

---
Typical unwanted loadings close-up

---
Clustering
We knew what types of samples we had, so we made artificial clusters out of them and then checked the silhouettes.
Cluster	Silhouettes
PC:	1-2	1-3	1-4	2-3	2-4	3-4	1-2-3	1-2-4	1-3-4	2-3-4	1-2-3-4
0	0.34	0.43	0.35	0.26	0.25	0.40	0.41	0.35	0.43	0.35	0.41
1	0.74	0.73	0.73	0.47	0.51	0.29	0.73	0.73	0.72	0.46	0.72
2	-0.19	-0.24	-0.23	-0.24	-0.28	-0.18	-0.19	-0.17	-0.22	-0.22	-0.18
Different PC projections of our samples and the corresponding silhouettes for the unmodified spectra.
Cluster 0 is natural kaolinites, 1 is artificial kaolinites, 2 is miscellaneous clay.
We can see that the silhouettes for some PC projections and for only cluster 1 are quite good.
An example PC projection of the samples within which the silhouette is measured

---
Clustering
Modified spectra received better silhouette scores. Here we will provide the best silhouettes, including the argon-helped data. Unmodified data is too unfitting to be included.
Cluster	Silhouettes
Spectra set:	No Ar, modified spectra				Ar-helped, modified spectra
PC:	1-2	1-2-4	1-4	1-2-3	3-4	2-4	2-3
0	0.48	0.46	0.42	0.48	0.39	0.6	0.55
1	0.86	0.82	0.81	0.79	0.8	0.71	0.7
2	-0.12	-0.12	-0.12	-0.14	-0.39	-0.35	-0.39

---
Conclusions
- In general, the analysis method is quite rapid, quite efficient and really portable.
- Miscellaneous clay rocks could not be categorized into one cluster and remain as a kind of a noise.
- Untreated spectra are not good for further analysis.
- Artificial kaolinites could be identified from the argon-less data set.
- Despite the argon dataset performing poorer than the argon-free one, it has potential for identifying not only artificial kaolinites but also the natural ones.